## Slide 1
Understanding Special Processes
Training Publication SPI-02
Rev 5
20 Dec 2025
by Konrad Burgoyne MIMF, FSPI

## Slide 2
Information
This training publication is provided for educational purposes and may be freely shared, copied and distributed. It is not subject to copyright restrictions.

## Slide 3
Content
Introduction
Requirement
What is a Special Process?
Risks
Standard Processes
Special Processes
Understanding the Three Tiers of Failure
Special Process Table
Specifications and Standards
Documented Information
Special Process Audit
Questions
Additional Reference Information

## Slide 4
Introduction
Aim
To broaden awareness and deepen understanding of special processes across all relevant roles.
Reason
Gaps in knowledge have been identified—many process owners and stakeholders do not fully understand special processes. Required controls may be ineffective.
Incentive
By increasing understanding and control of special processes, we can reduce operational risk, achieve product conformity and ensure compliance with AS9100 and customer requirements.

## Slide 5
Validation & Verification
To better understand the content of this training on special processes;
The term validation can be interpreted as interchangeable with testing.
The term verification should be understood as the process of checking, measuring or monitoring.
*The ISO9000 definitions of validation and verification can be found at the end of this slide pack.
Terminology

## Slide 6
ISO9000:2015(E) 3.4.1 Process, Note 5:
A process where the conformity of the resulting output cannot be readily or economically validated is frequently referred to as a “special process”.
What is a special process?

## Slide 7
The process produces a product or changes a product; where one or more of the product characteristics cannot be directly measured to verify conformity.
Therefore, the process must be periodically validated, typically using a representative test piece that is processed under the same conditions and then destructively tested.
Periodic testing ensures that the process consistently produces conforming product
What does that mean?
“Unseen, but critical”.

## Slide 8
If the process is not operated correctly or validation is ineffective, products could be produced with undetectable nonconformities. Leading to failure at a later stage while in service.
E.g. Adhesion failure, unpredicted corrosion, stress corrosion cracking, delamination, sub-critical grain growth, PCB dry joints, creep and stress rupture, shear failure etc.
What are the risks?

## Slide 9
PROCESS ACTIVITY
Process Verification by Product Validation
ACT
PLAN
CHECK
DO
PRODUCT OUTPUT
Production Process Verification (FAIR)
Product Validation (Testing)
INPUT
Process can be verified by testing, measuring and monitoring output key characteristics
Standard Process

## Slide 10
A machined or made part can be validated by direct measurement of dimensions against the drawing or design data. Therefore the (production) process can be verified.
Verification data can be included into a First Article Inspection Report (FAIR) for example.
Example of a (Standard) Process
Design Drawing
Nonconformities can be easily identified
AS9100
8.5.1.3 Production Process Verification
The organization shall implement production process verification activities to ensure the production process is
able to produce products that meet requirements.

## Slide 11
Example of a Special Process
A painted part can be verified by direct measurement of coating thickness. However, other characteristics such as poor adhesion due to insufficient process control might not be detected until failure occurs in service.
AS9100
8.5.1.2 Validation and Control of Special Processes
For processes where the resulting output cannot be verified by subsequent monitoring or measurement, the
organization shall establish arrangements for these processes including, as applicable:
a. definition of criteria for the review and approval of the processes;
b. determination of conditions to maintain the approval;
c. approval of facilities and equipment;
d. qualification of persons;
e. use of specific methods and procedures for implementation and monitoring the processes;
f. requirements for documented information to be retained.
Characteristics can be implied!
For example, a painted product specification might not explicitly state that the paint must remain adhered—but that requirement is inherently expected.
Nonconformities cannot be easily identified

## Slide 12
PROCESS ACTIVITY
Product Verification by Process Validation
ACT
PLAN
CHECK
DO
Process Validation (Testing)
INPUT
PRODUCT OUTPUT
Product can be verified by periodic testing (validation) of the process
Special Process

## Slide 13
Intent
Lack of intent to perform process validation—often due to a misunderstanding of requirements or the perception that validation is an unnecessary cost or burden.
Implementation
Intent is present and process requirements are understood; however, effective training and/or process validation have not been implemented.
Effectiveness
The special process is validated through defined controlled conditions but the process is not always followed correctly during normal production.
To fully understand the potential serious consequences of inadequate process control, refer to the additional reference information provided at the end of this slide pack.
Understanding the Three Tiers of Failure

## Slide 14
Special Processes Table
Aerospace, Space & Defence Special Processes Incorporated in Manufacturing |  | 
Welding | Chemical Processing | Electronics
Rotational Friction / Inertia Welding, Torch / Induction Brazing, Flash Welding & Laser Welding, Electron Beam Welding, Resistance Welding, Fusion Welding & Evaluation of Welds | Electroplating, Electroforming, Electroless Plating, Anodising, Chemical Conversion Coatings, Passivation, Painting & Dry-Film, Surface Enhancement, Etching & Chemical Cleaning | Printed Circuit Board (PCB) Manufacture, PCB Assembly (Incl. Soldering), Cable and Harness Assemblies, Conformal Coating, Battery Cell Manufacture & Array Assemblies
Composites | Elastomer Seals | Heat Treatment
Prepreg, Adhesive Bonding, Resin Film Infusion (RFI), Metal Bonding, Core Processing, Liquid Resin Processing & Compression Moulding | Plate Seals, Fabric / Textile Reinforced Seals, O-Rings & Moulded Shapes | Brazing, Aluminium Heat Treating, Carburizing, Nitriding, Hot Isostatic Pressing, Induction Hardening & Sintering
Materials Testing & Inspection | Nonconventional Machining | Non-destructive Testing
Chemical Analysis, Mechanical Testing, Metallography, Micro Indentation Hardness Testing, Corrosion Testing, Fastener Testing, Physical Testing, Thermal Testing & Coordinate Measuring Machines (CMM) | Electrochemical Machining, Electrochemical Grinding, Electrical Discharge Machining, Laser Beam Machining, Laser Part Marking & Spark Erosion Grinding | Penetrant Flaw Detect, Anodise Flaw Detect, Magnetic Particle Inspection, Ultrasonic Testing, Radiographic Inspection Testing & Eddy Current Inspection Testing
Additive Manufacturing |  | 
Directed Energy Deposition (DED) | Powder Bed Fusion (PBF) | Sheet Lamination (SHL)
Laser Engineered Net Shaping (LENS), Electron Beam Additive Manufacturing (EBAM), Wire Arc Additive Manufacturing (WAAM) | Selective laser sintering (SLS), Selective laser melting (SLM), Direct metal laser sintering (DMLS), Electron beam melting (EBM), Selective heat sintering (SHS) & High-speed sintering (HSS) | Laminated object manufacturing (LOM), Selective lamination composite object manufacturing (SLCOM), Plastic sheet lamination (PSL), Computer-aided manufacturing of laminated engineering materials (CAM-LEM), Selective deposition lamination (SDL), Composite-based additive manufacturing (CBAM) & Composite fiber (SLCOM)
Material Extrusion (MEX) | Material Jetting (MJT) & Binder Jetting (BJT) | Vat Photopolymerization (VPP)
Fused deposition modeling (FDM) & Fused filament fabrication (FFF) | PolyJet, Nanoparticle jetting (NPJ), Drop on demand (DOD) | Stereolithography (SLA), Digital light processing (DLP) & Continuous digital light processing (CLIP)

## Slide 15
Special Processes Specifications & Standards
Examples of Special Process Standards & Specifications |  | 
Welding | Chemical Processing | Electronics
ISO 24394, Def Stan 03-34, Def Stan 08-39, ISO 10042, ISO 3834, ISO 2553, AWS D17, AWS B5.2 | MIL-PRF-8625, MIL-DTL-5541, AMS 2700, AMS-QQ-N-290, ASTM B545, ISO 2081, ISO 4042, AMS 03-11, AMS 2454, Def Stan 03-32 | IPC J-STD-001, IPC-A-600, IPC-A-610, IPC-A-620, IPC-A-630, IPC-CC-830
Composites | Elastomer Seals | Heat Treatment
ASTM E2981, ASTM D6856 ASTM D7745, AMS 3914, AMS 6885, AMS 3961, ISO 21368 | ISO 27996, AS4716, AS3569 | AMS 2750, AMS 2759, AMS 2769, AMS 2770, AMS 2771, AMS 2772, AMS 2773, AWS A5.31, AWS C3.7, ISO 13585
Materials Testing & Inspection | Nonconventional Machining | Non-destructive Testing
ISO 22826, ASTM E103, ASTM E1842, ISO 6892, ASTM E1004, AMS2658, ASTM B-117, ISO 15530-3, ASME B89, ISO 898-1, ISO 3506-1, ASTM F606 | AMS2548, ASTM DL MNL56, VDI 3400, BS 2634-2 | ASTM E1417, ISO 3452, ISO 5579, EN 4179, ISO 9712, ISO TS 11774, ASTM E3166, ASTM E165, ASTM E1209, ASTM E709
Additive Manufacturing |  | 
DNV-CG-0197, ISO/ASTM 52904, ASTM 52927, ISO 17295, ASTM 52950, ASTM 52919, ASTM 52930, ASTM 52910, ASTM 52900, ASTM F3635, AWS D20.1, ASTM DL STP1631, NACE AMPP TR21522, ASTM F3554, AMS7005, ASTM F3413 |  | 
Process Specifications
Include process control criteria and validation methods and frequency

## Slide 16
Special Process Documented Information
Best Practice Documentation for Process Control
To ensure effective process control, documentation should follow best practices meeting EN9100 8.5.1.2 and include the following components:
Top-Level Process Control Document: Outlines the overall requirements and structure of the process control system.
Special Process Library: A comprehensive list or library of all special processes performed.
Special Process Documentation: Each special process should have a dedicated document titled Special Process Operation, Validation & Process Control. This document must extract all relevant specifications and define:
  Detailed process control criteria
  Validation methods and their frequencies
Process Control & Validation Records: Maintain records of process control activities and periodic testing.
Process Flow Charts: Each special process should have an associated flow chart. This may be included in the job card or ‘traveller’.
Audit Criteria Checklist: Each special process must include a checklist of audit criteria for use during periodic audits.
ISO 9001 / EN 9100
Top Level Special Processes Document
Special Processes List
Special Process Operation, Validation & Process Control
Special Process Validation & Process Control (Periodic Testing) Record
Special Process Audit Criteria
Special Process Flow Chart
Job Card
Traveller / Production Record
Audit Scope
All documentation, records, equipment and the operation of the process

## Slide 17
Special processes must be periodically audited by specification checklist to ensure compliance. Audits will verify process validation. Audits should confirm:
Intent: Confirmed by document review.
Implementation: Confirmed by reviewing equipment, environment, qualification, calibration, certification and validation records.
Effectiveness: Confirmed by reviewing process by witnessing, interview and objective evidence verification.
Special Process Audit

## Slide 18
Questions?

## Slide 19
Additional Reference Information
The following slides present significant failures—many resulting in fatalities—linked to inadequate control of special processes.
These cases underscore the critical importance of effectively managing special processes and the severe consequences when nonconformities go undetected until a failure occurs later in service.

## Slide 20
Welding Related Failures
Incident | Year | Location | Fatalities | Role of Poor Welding | Details
Alexander L. Kielland Platform | 1980 | North Sea | 123 | Poor welding and inadequate NDT | Fatigue crack in a 6mm weld initiated by improper weld technique and poor NDT inspection
Piper Alpha Oil Rig Disaster | 1988 | North Sea | 167 | Poor welding and improper installation of a pipe plug | Gas leak triggered explosions; maintenance and weld integrity failures contributed.
I-35W Bridge Collapse | 2007 | Minneapolis, USA | 13 | Poor welding contributed to fatigue cracks | Weld defects weakened gusset plates, leading to sudden collapse.
Ghislenghien Gas Explosion | 2004 | Belgium | 24 | Weak pipeline welds | Welding deficiencies contributed to explosion after accidental damage.
BP Texas City Refinery Explosion | 2005 | Texas, USA | 15 | Substandard welding and maintenance | Poor welding inspections and degraded piping contributed to vapor leak and ignition.
San Bruno Gas Pipeline Explosion | 2010 | California, USA | 8 | Faulty and undocumented welds | Pipeline welds failed under pressure due to internal flaws and lack of testing.

## Slide 21
Composite Related Failures
Incident | Year | Location | Fatalities | Root Cause in Composite Materials | Details
SpaceShipTwo VSS Enterprise Crash | 2014 | California, USA | 1 | Structural failure during descent (composite control surfaces) | Premature unlocking of the feathering system in a composite structure led to in-flight breakup. Composite delamination was studied as a factor in fragmentation.
Scilly Isles Agusta A109 Helicopter Crash | 1983 | UK | 3 | Rotor blade failure (composite delamination) | Investigators found fatigue and delamination in composite rotor blades, leading to loss of control.
Carbon Fiber Racing Car Crash (Le Mans) | 1999 | France | 1 | Improper bonding and poor crashworthiness of composite tub | Composite monocoque failed to absorb crash energy as designed. Inadequate layup and bonding contributed to fatal injuries.
American Airlines Flight 587 | 2001 | New York, USA | 265 | Failure of composite vertical stabilizer | Overstressing of carbon fiber rudder attachment lugs (composite delamination and brittle failure); poor bonding and load transfer integrity.
Wind Turbine Blade Collapse (Maintenance Accident) | 2013 | Netherlands | 2 | Catastrophic failure of composite blade during repair | Internal defects and poor maintenance led to a blade snapping during technician access. They fell to their deaths.

## Slide 22
Heat Treatment Related Failures
Incident | Year | Location | Fatalities | Heat Treatment Root Cause | Details
China Eastern Airlines Flight 5735 Crash | 2022 | China | 132 | Suspected heat treatment or structural fatigue in elevator components (under investigation) | Investigators analyzed possible improper heat treatment on control surfaces that may have led to catastrophic control failure.
US Military Helicopter Crash (Main Rotor Failure) | 1986 | USA | 5 | Poor heat treatment of rotor spindle | Crack initiated due to improperly tempered steel rotor spindle; led to in-flight failure of the main rotor system.
Ford Pinto Fuel Tank Fires | 1970s | USA | 27 | Poorly heat-treated structural parts near fuel tank | Frame parts were brittle due to inadequate heat treatment; contributed to tank rupture and fires in rear-end collisions.
Queensland Mining Drill Rod Failure | 2009 | Australia | 1 | Drill rod fractured due to improper tempering | Drill rod snapped under stress; fractured segment struck and killed the operator. Metallurgical analysis showed inadequate quenching and tempering.
Railway Axle Failure – Eschede Train Disaster | 1998 | Germany | 101 | Undetected fatigue crack in poorly heat-treated axle | Heat treatment defects led to fatigue crack growth; the wheel disintegrated at high speed, causing derailment.
Aircraft Engine Turbine Blade Failure | 2000s (multiple incidents) | Global | Several | Creep and fatigue due to improper heat treatment | Inconsistent heat treatment on nickel-based turbine blades led to early failure, including in one instance causing uncontained engine failure and fatalities.

## Slide 23
Chemical Processing Related Failures
Incident | Year | Location | Fatalities | Root Cause Involving Surface Coatings | Details
Valero Texas City Refinery Explosion | 2005 | Texas, USA | 15 | Failure of protective coatings on pipes and tanks | Protective coatings degraded, allowing corrosion under insulation (CUI) to go undetected, contributing to vapor release and explosion.
BP Texas City Refinery Disaster | 2005 | Texas, USA | 15 | Coating failure on tanks and pipes | Poor maintenance of anti-corrosion coatings led to unnoticed thinning of walls, allowing hydrocarbons to escape.
I-35W Bridge Collapse | 2007 | Minneapolis, USA | 13 | Coating degradation leading to corrosion fatigue | Degraded paint/coatings allowed moisture ingress, accelerating corrosion of steel bridge components, contributing to fatigue failure.
Formosa Plastics Explosion | 2005 | Illinois, USA | 5 | Coating breakdown on corroded piping | Failed anti-corrosion coating contributed to undetected wall thinning in high-temperature piping system.
Corrosion Under Insulation (CUI) Incidents – Offshore Rigs | Ongoing | North Sea / Gulf of Mexico | Multiple fatalities across years | Poor surface prep or failed coatings under insulation | Inadequate coatings beneath insulation led to pipe corrosion, leaks, and fire/explosion risks in hydrocarbon processing areas.
Incident | Year | Location | Fatalities | Anodizing-Related Root Cause | Details
Bell 206 Helicopter Crash (Tail Rotor Failure) | 1995 | Australia | 2 | Poor anodizing led to corrosion and cracking of tail rotor yoke | Improper anodizing and sealing failed to protect aluminum rotor parts from corrosion; initiated fatigue cracking that caused in-flight separation.
Cessna Aircraft Structural Failure (Various cases) | 1990s–2000s | USA | Multiple | Inadequate anodizing in wing spars or fittings | FAA issued Airworthiness Directives on Cessna aircraft after finding corrosion in anodized parts due to improper processing. Some cases led to inflight breakup or crashes.
Ultralight Aircraft Crash (Rudder Failure) | 2014 | UK | 1 | Aluminum rudder hinge corroded due to failed anodic coating | Anodizing was improperly applied and sealed; corrosion propagated through the hinge, which failed mid-flight.
Military Drone Crash (Unmanned Aerial Vehicle) | 2009 | USA | 0 (equipment loss only) | Poor anodizing caused delamination and corrosion on control surfaces | While not fatal, the incident led to increased scrutiny of anodizing quality in UAV airframes.
General Aviation Crashes (FAA ADs issued) | Ongoing | USA | Multiple | Stress corrosion cracking in anodized aluminum landing gear or fittings | Improper anodizing (e.g., poor sealing, wrong electrolyte) made aluminum vulnerable to chloride-induced stress corrosion cracking (SCC).

## Slide 24
PCB Related Failures
Incident | Year | Location | Fatalities | Root Cause Related to PCB | Details
Toyota Sudden Unintended Acceleration | 2000s | USA & global | 89 | Suspected cracked solder joints and PCB failures in electronic throttle control | Independent investigations (NASA, university researchers) pointed to possible PCB micro-cracks or tin whiskers causing signal faults in throttle control modules.
Therac-25 Radiation Overdoses | 1985–1987 | USA & Canada | 6 | Software and hardware race condition involving poor PCB circuit design | A combination of software flaws and inadequate interlocks in the PCB allowed lethal overdoses of radiation in cancer treatment machines.
Apollo 1 Fire (Command Module) | 1967 | USA | 3 | Faulty wiring and possible PCB-related short circuits in oxygen-rich environment | While mainly attributed to wiring and flammable materials, PCB assembly and poor electrical isolation were cited as compounding risks.
Boeing 737 MAX Crashes (Lion Air & Ethiopian Airlines) | 2018–2019 | Indonesia & Ethiopia | 346 | Suspected poor-quality angle-of-attack sensor circuitry | While not officially blamed on PCBs, electronics controlling the MCAS system (which misfired) included critical circuit boards. Poor redundancy and failure detection contributed to the crashes.
Medical Device Failures (Implantable Defibrillators, Pacemakers) | 2000s–2010s | Global | Multiple | PCB delamination, cracked solder joints in defibrillators and ICDs | Companies like Guidant and Medtronic issued recalls after internal PCBs failed under stress, leading to devices not shocking or failing silently.
Airbus A330 Pitot Heater PCB Fire Incident (non-fatal) | 2011 | USA | 0 (near-miss) | PCB manufacturing defect caused overheating and cockpit smoke | Pitot tube heating PCB had a solder defect, leading to a fire warning mid-flight. Landed safely, but led to global inspections.

## Slide 25
Additive Manufacturing Related Failures
Incident | Year | Location | Fatalities | Root Cause Related to AM Process | Details
Medical Implant Failure (Hip Replacement) | 2010s | Global | Several reported patient deaths | Porosity and defects in 3D-printed titanium implants leading to premature failure | Poor process control caused internal voids and weak microstructures; implant fractured or loosened, causing life-threatening complications.
Aerospace Component Failure | 2018 | USA | Fatalities in crash incidents (confidential) | Incomplete fusion and residual stress in AM turbine parts | Poor powder quality and layer bonding defects resulted in catastrophic failure of engine parts during flight.
Automotive Crash Due to 3D-Printed Structural Part Failure | 2020 | Europe | 2 | Improper AM parameters causing weak bonding in load-bearing parts | A structural suspension part failed during operation due to delamination and porosity from faulty AM process control.
Military UAV Crash | 2019 | Classified | Fatalities unknown | Defects in additive-manufactured control surfaces | Poor quality control led to cracks and delamination under stress, causing loss of vehicle control.
Dental Implant Failure Leading to Fatal Infection | 2015 | USA | 1 | Contaminated AM process and defective implant surfaces | Microbial contamination during AM and poor surface finish led to implant failure and severe infection.

## Slide 26
NDT Related Failures
Incident | Year | Location | Fatalities | NDT Root Cause | Details
San Bruno Gas Pipeline Explosion (PG&E) | 2010 | California, USA | 8 | Flawed or falsified NDT and inspection records | A defective weld in a pipeline seam went undetected; subsequent explosion destroyed homes and killed residents. Investigation revealed incomplete or manipulated NDT documentation.
Eschede Train Disaster (Germany) | 1998 | Germany | 101 | Fatigue crack missed by NDT in wheel hub | Routine NDT failed to detect a growing fatigue crack in a steel wheel; disintegration at high speed led to a high-speed derailment.
Piper Alpha Oil Rig Disaster | 1988 | North Sea | 167 | Missed weld cracks and fatigue damage during inspection | NDT deficiencies allowed fatigue cracks in pipes and flanges to remain in service, contributing to gas release and explosion.
Aloha Airlines Flight 243 | 1988 | Hawaii, USA | 1 | Visual-only inspection missed widespread fuselage cracks | Widespread corrosion fatigue cracking in the aircraft’s composite fuselage skin (near lap joints) went undetected due to lack of advanced NDT like eddy current or ultrasonic testing.
Boeing 737 Rudder Hardover Incidents | 1990s | USA | 2 | Inadequate NDT in manufacturing and inspection of actuator parts | Improper NDT allowed latent defects in hydraulic rudder control components to go undetected. Multiple incidents occurred, including fatal crashes.

## Slide 27
Elastomer Seal Related Failures
Incident | Year | Location | Fatalities | Root Cause Related to Elastomer Seal | Details
Deepwater Horizon Oil Spill | 2010 | Gulf of Mexico | 11 | Blowout preventer seal failure (elastomer seal degradation) | Failure of elastomer seals in the blowout preventer allowed uncontrolled oil and gas release, causing explosion and fatalities. Seal materials failed under extreme conditions.
Bhopal Gas Tragedy | 1984 | India | 3,787 | Seal failure in gas storage tanks and pipelines | Aging and chemically degraded elastomer seals contributed to methyl isocyanate gas leakage, leading to one of the worst industrial disasters.
Space Shuttle Challenger Disaster | 1986 | USA | 7 | O-ring (elastomer seal) failure in solid rocket booster | Cold temperatures caused O-ring seals to lose elasticity, allowing hot gases to escape and destroy the shuttle.
Chevron Richmond Refinery Fire | 2012 | California, USA | 1 | Elastomer seal failure on piping system | Seal degradation led to hydrocarbon release and fire during maintenance.
Titan Submersible Implosion (Investigation ongoing) | 2023 | Atlantic Ocean | 5 | Possible seal failure in pressure hull (composite and elastomer seals) | Initial hypotheses include failure of seals used to maintain pressure integrity, though investigation continues.
Hydraulic Failure in Construction Equipment | Various | Global | Several | Elastomer seal extrusion and rupture in high-pressure hydraulic lines | Sudden loss of hydraulic pressure caused loss of control and fatal accidents involving heavy machinery.
Chemical Plant Explosion Due to Valve Leak | 1999 | USA | 4 | Degraded elastomer seals in critical valves | Seal failure caused release of flammable chemicals, igniting explosion.

## Slide 28
Nonconventional Machining Related Failures
Incident | Year | Location | Fatalities | Root Cause Related to Nonconventional Machining | Details
Aeroengine Turbine Blade Failure | 1990s–2000s | Global | Multiple (various incidents) | EDM-induced microcracks and residual stresses in turbine blades | Poor EDM process control caused microcracks that propagated during service, leading to blade failure and fatal accidents.
Titanium Implant Failure | 2010s | Medical device industry | Several | Laser machining-induced microstructural changes weakening implant | Poor laser machining parameters led to weakened implant parts that failed inside patients, causing deaths due to implant collapse.
Military Missile Guidance System Malfunction | 2000s | USA | Classified (likely fatalities) | Poor waterjet cutting causing dimensional inaccuracies | Dimensional errors led to system failures in missiles, causing accidental explosions or mission failure with casualties.
Aerospace Structural Part Fracture | 2015 | Europe | 2 | Ultrasonic machining induced subsurface damage | Subsurface cracks went undetected, causing structural failure in aircraft control surfaces.
Nuclear Reactor Component Failure | 1990s | USA | Potential fatalities (near misses) | Poor EDM machining of fuel assembly parts | Residual stress and cracking due to poor machining practices threatened reactor safety.

## Slide 29
Corrosion Related Failures
Incident | Year | Location | Fatalities | Role of Corrosion | Details
Silver Bridge Collapse | 1967 | West Virginia–Ohio, USA | 46 | Stress corrosion cracking of eyebar chain link | Corrosion-induced crack led to failure of suspension chain, collapsing the bridge during rush hour.
Mianus River Bridge Collapse | 1983 | Connecticut, USA | 3 | Severe corrosion of pin-and-hanger assembly | Rainwater caused hidden corrosion in load-bearing joints; lack of inspection allowed degradation to go unnoticed.
Aloha Airlines Flight 243 | 1988 | Hawaii, USA | 1 | Widespread corrosion and fatigue cracking in fuselage | Saltwater corrosion led to explosive decompression; aircraft had reached high cycle count without sufficient inspection.
Mexico City Gas Explosion | 1984 | Mexico | 500 | Corrosion in LPG pipelines | Underground LPG pipes corroded, allowing gas to leak and accumulate, eventually igniting in a massive explosion.
ValuJet Flight 592 (indirect) | 1996 | Florida, USA | 110 | Oxygen generators corroded & mishandled | Improperly stored and corroded oxygen canisters ignited in the cargo hold. Though not purely metal corrosion, metal degradation played a role.
Minneapolis Water Main Collapse | 1986 | Minnesota, USA | 1 | Pipe corrosion | Corroded water pipe burst, collapsing a road and a passing vehicle into the hole.

## Slide 30
Terms – Verification & Validation
ISO9000:2015(E) 3.8.12
Verification - confirmation, through the provision of objective evidence, that specified requirements have been fulfilled.
ISO9000:2015(E) 3.8.13
Validation - confirmation, through the provision of objective evidence, that the requirements for a specific intended use or application have been fulfilled.
Verification is like checking that your car was built exactly according to the blueprint. (Review test results against requirement)
Validation is taking the car for a test drive to ensure it actually drives well and meets your needs.
(Perform test)
Aspect | Verification | Validation
Definition | "Are we building the product right?" | "Are we building the right product?"
Purpose | To ensure the product meets design specifications and requirements. | To ensure the product meets user needs and intended real-world use.
Focus | Internal consistency with requirements, design, and implementation. | External correctness for the actual end-user or operational environment.
When Performed | During and after development (often in stages). | After verification, typically before release or deployment.
Examples | - Code review matches design- Circuit built to spec- Dimensions match drawing | - End user test shows system meets expectations- Aircraft simulator confirms flight performance- Medical device works properly on a patient
Methods | Inspections, walkthroughs, tests, simulations | Field testing, user acceptance testing (UAT), pilot trials
Driven by | Technical requirements/specifications | Customer expectations or use cases

## Slide 31
Revision Control
sp-i.org
email@sp-i.org
Rev | Date | Change | Author
1 | 10 Sep 2016 | Established training slide pack with special processes guidebook | Konrad Burgoyne
2 | 25 Jan 2018 | Addition of special processes table | Konrad Burgoyne
3 | 22 Nov 2020 | Addition of process specification example table | Konrad Burgoyne
4 | 10 Jun 2022 | Addition of special process related failure tables | Konrad Burgoyne
5 | 20 Dec 2025 | Rebranding update to document | Konrad Burgoyne